## Slide 1: Composite Flexible Pipelines
Jim Latto & Dr Vineet Jha
GE Oil & Gas

## Slide 2: Next Generation Composite Flexible Risers
30% Lighter
20% Savings on total installed cost
Deeper Water & Higher Pressures
FHC in 3000m water depth

## Slide 3: Flexible Riser Construction
Carcass – Inner metallic layer prevents collapse due to hydrostatic pressure
Fluid Barrier – Chemically resistant polymer boundary for conveyed fluids
Pressure Armour – Interlocked metallic layer resists internal pressure loads
Tensile Armour – Provides axial support for the entire riser
Insulation Layer – Prevents excessive heat loss in bore fluids during operation
Outer Shield – Protects the pipe against seawater ingress and external damage
20%
5%
35%
40%
1%
4%
190 kg / m
3km - 8”ID - 12ksi
Layer Weight
Notes: I would like to give you a little more information on how they work.
A flexible pipe is essentially a composite itself, made up of different elements that each perform a specific function.
[layer explanation – function only with metallic / non metallic]
The required overall capability of these pipelines depends on the specific field conditions under which they will be operated. These conditions in turn dictate the specification for each functional layer, creating a truly bespoke design.
Because each layer is bespoke, we were able to, and indeed took the opportunity to make an incremental change to one specific layer that gives us the most significant impact to the overall pipe performance, and perhaps more importantly, this allowed us to address both of our goals to reduce overall costs and increase capability at the same time without completely re-designing a trusted and proven product.
To give an example that is relevant to work we have been carrying out specifically for the GOM field conditions, [click] PIPE DETAIL ON SLIDE….. We have an 8” UDW UHP pipe. The weight distribution of the layers within this pipe are as follows….
As expected, the metallic layers within a pipe contribute to the lion share of the weight. One of the heaviest layers in this design is the internal pressure armour. This internal pressure armour is the key layer with regard to the upper pressure limit of subsea flexibles and also effects the requirements for the tensile armour layer. The heavier we make the pressure armour, the heavier we have to make the tensile armour to cope with the weight …. [slide]

## Slide 4: Composite Pressure Armour
4
Metallic FlexLok
Zeta section wire
Heavy construction
Ultra high pressure
Sour service
Metal / metal contact
Sacrificial polymer layer
High pressure capacity
Well known and trusted materials
State of the art manufacturing
Simplified design
Optimised material usage
Flexible and fatigue resistant
Mature and proven end terminations
Notes: Make 1 round image instead of two
Reduce text

## Slide 5
30% Increase in Reel Capacity
Reduced Mobilisation Cost & Time
Reduced Shipping Cost
Reduced Installation time & Ancillaries
Platform Optimisation & FHC
20% reduction in total installed cost
when able to move from lazy wave configuration to free hanging catenary
Conventional Flexible Pipe
Composite Flexible Pipe

## Slide 6
2010
2013
2014
2015
2016
2017
2018
2019
Coupon properties and
RPSEA Award
Ageing and RGD
completed
OTC-2014 25393
Defect detection
monitoring system developed
IHTEC 2014
DTR and TCR
sample testing
Full-scale testing and qualification completed
GE’s
Bonded CPA concept conceived
Compression and
TDP analysis
OMAE 2014 23579
Mid-scale testing
completed OTC 2015
25753
First full-
scale ATL manufacturing
module procured
Static testing and
manufacturing results
OTC 2013 24160
Full-scale ATL module commissioned
Completed
In progress
Final Target
Program Timeline

## Slide 7: Multi-scale Qualification
Non-generic
Generic
Database
Structural Features
Coupons
(e.g., flat coupons)
Elements
(e.g., as mfg. composite)
Details
(wire/composite features)
Sub-components
(mid-scale pipe)
Components
(full-scale pipe)
Flexural/Bending
Hoop / Pressure
Internal pressure
Notes: # Slide 8
In present case, I will quickly summarise two most important properties for Composite pressure armour i.e Hoop pressure resistance and Flexural of ability bend this layer and transport this in same way as current flexible.
Pyramids shown here represent number of testing and can vary from 1000 at bottom to single digit at full scale testing.
You start from testing material received in Tape from material supplier, followed by testing of plates …
Next level of testing involves pipe cut offs. Finally this is matched up Mid-scale testing where actual pipe with all or some layers is tested with or without end fitting.
Once enough confidence has been built final verification is carried out at full scale
If you image third dimension to this triangle it is modelling tools.
Given the time constraints I will be discussing mid-scale and full scale pipe components in detailes

## Slide 8: Burst Performance: Mid-scale Pipe Testing and Modelling
Burst tests – 12 ksi design pressure with analysis model validation
Proven burst performance for 24 ksi /~160 MPa
FE modelling was used to accurately predict failure point
Axial strain
Hoop strain
Notes: #Slide 9
Given the time I will discuss Key Mid-scale and Full scale testing will be discussed in present presentation.
Starting with Burst.
As part of RPSEA programme we designed a mid-scale burst rig, this pipe has carcass polymer barrier and composite layer and has swagged seal arrangement.
We model swagged seal are working out burst pressure, stress in seal ring area radial and circumferential and axial stress.
The actual burst test was performed with pipe busting at 160 Mpa.
This burst pressure was predicted accurately used modelling tools used.

## Slide 9: Mid-scale: Rotating Bend Fatigue Testing
Mid-scale rotating bending fatigue.
Low strain, high fatigue cyclic loading.
Captures the tri-axial stress state.
Cross-section of sample after 1 million cycles in rotating bend fatigue rig.
Both composite and interface layers were checked before and after testing.
Notes: # Slide 10
WE regards to bend fatigue we manufactured several a mid scale sample. A 10 inch size pipe with carcass polymer barrier and composite layer is shown here. This sample was assembeled in rotating bend fatigue rig end applying strain
Strain cycle mirrored the actual life cycle on pipe with high strain cycle followed by 1 million cycle at 1 percent strain.
This loading cycle mirrors 25 years of life of composite riser.
A cross section image has been shown in presentation. It shows the interface and composite layer remaining intact after exposure high strain and Low strain fatigue cycle

## Slide 10: Large-scale Dynamic Testing - Combined Loading Testing
Inside diameter | 254.00 mm
Max tension | 500 kN
Storage bend radius | 3.9m
Operating bend radius | 3.9m
Weight empty in air | 77.16 kg/m
S/W filled in air | 133.34 kg/m
A full-scale dynamic testing rig (DTR) sample will consist of carcass, barrier, composite pressure armor, tensile armor and wear layers.
In addition to testing tensile-fatigue-critical tensile amour layers, the effect of bending loads on the composite pressure layer can be studied.
Additionally, the effect of the interaction between the tensile and composite pressure armor will be captured.
Changes in friction factor and its effect will be studied.
Full-scale dynamic fatigue test rig at ETA International
Full-scale pipe and test parameters
Notes: ?? # slide 11.
AS part of Rpsea programme we build a full scale 12 m sample with all layers shown. i.e carcass polymer composite pressure armour, tensile armour wire and full end fitting. This sample is suspend in DTR rig shown here. This rig simulates the tension, bending moements seen by pipe. Additonally pressure cycle and temperature cyclcling are mirroooned to respresent life cycle of comppoasite pipe. This testing is due to complted by Aug 2016.
This will verify results of Small, mid scale roatating bend fatigue resul;ts. Also, inter- larer interaction and modelling ascpts have been verfired.
????

## Slide 11: System Optimisation
Top end tension reduction
Optimise platform capacity vs no. of risers
Simpler bend stiffener design due to less onerous requirements
Reduced buoyancy requirements
Installation time saving
Reduction in weight & top tension allows increased free hanging catenary length
CPA optimised to meet TDP demands
Reduced overall pipe diameter improves dynamic stability

## Slide 12: Capability – Composite Pressure Armour
8” ID
5000 psi
10000 psi
20000 psi
Pressure Capacity
Pressure Armour Thickness
Single material qualification to cover entire pressure range

## Slide 13: Summary
Next Generation Composite Flexible Risers
30% Lighter
20% Savings on total installed cost
Deeper Water
Higher Pressure
Simpler configuration