| Project Code | R166 | Project Sponsor | Alberto Matucci |
| --- | --- | --- | --- |
| Project Name | Composite Flexible Pipe | Project Manager | Jim Latto |
| WBS | R166.B.5.C.5.1 | Principal Engineer | Neville Dodds |
| Document Ref | R166Exxx | Owner | Brendan O’Donnell |
| Revision | P | Revision Date | 19/01/17 |
| Work Package Title | Small-scale - Mechanical / Physical Categorisation - Start of Life (API Standard) |  |  |

# Work Package Summary

|  | Description of test / group of Tests within work package. Why is the test / group of tests needed? What will data generated from this test / group of tests be used for? |
| --- | --- |

This work package contains all mechanical and physical coupon level testing for materials used in composite pressure armor in an unaged condition.  Categorizing these properties is a qualification requirement and will be verifies / checked by the IVA. These properties, if required, when required will also be used as inputs to higher level testing. modelling, design and analysis.

# Work Package Deliverables

|  | Specific deliverables, numbered with specific references to the project WBS and any relevant documentation that raises the requirement (API / DNV / FMECA Item etc.) |
| --- | --- |

| WBS | Task Name | Pipe FMECA Ref | EF FMECA Ref |
| --- | --- | --- | --- |
| R166B.1615 | Bend Properties | 1.4, 5.2, 5.8, 5.10 |  |
| R166B.1620 | Compression | 2.1, 2.2, 5.10 | 3.2, 4.1 |
| R166B.1630 | Friction Factor | 2.1, 2.2 |  |
| R166B.1640 | Resistance to Creep | 3.1, 3.2, 4.1 | 3.2, 4.1 |
| R166B.1650 | Tensile Properties | 1.2, 1.3, 1.4, 3.1, 3.2, 3.5, 4.1, 5.8, 5.10 |  |
| R166B.1660 | Stress Relaxation Properties | 3.1, 3.2, 4.1, 5.3 | 3.2, 4.1 |
| R166B.1670 | Compression Properties | 3.1, 3.2, 5.10, 5.11 |  |
| R166B.1680 | Hydrostatic Pressure Resistance | 3.1 |  |
| R166B.1690 | Abrasion Resistance | 3.1 |  |
| R166B.1700 | Density | 3.1 |  |
| R166B.1710 | Flexural Fatigue | 3.1, 3.3, 3.4, 5.6, 5.7, 5.8, 5.10 |  |
| R166B.1720 | Notch Impact Test | 3.1, 3.4, 5.5, 5.6 |  |
| R166B.1830 | Tensile Fatigue | 3.3, 5.6, 5.7, 5.8, 5.10 |  |
| R166B.1850 | Creep Rupture | 5.1, 5.3 |  |
| R166B.1900 | Split D Testing | 5.12 |  |
| R166B.1920 | Inter Layer Friction |  | 3.2 |

# Work Package Links / References

|  | Reference documents and links to documents (Where possible) Examples: API 17xx, DNV RP xx, FMECA - R166Exxx, Procedure - WSI ENGxxx, Design and business reviews |
| --- | --- |

1.  FMECA - Hyperlink

2.  DNV RP's- Hyperlink

3.  API- Hyperlink

4.

5.

6.

7.

8.

9.

10.

11.

12.